## Slide 1
METSAPP
Metal supported SOFC technology for stationary and mobile applications
(GA number 278257)
Niels Christiansen
Topsoe Fuel Cell A/S

## Slide 2: Project & Partnership
  General Overview
  Metal supported SOFC technology for stationary and mobile applications
  3 years (2012-2014)
  Budget
  Total: 7.886.781 EURO
  EU contribution: 3.396.470 EURO
  Danish top up support: 1.034.732 EURO
  Consortium
  Topsoe Fuel Cell A/S (DK)
  Sandvik Materials AB (SE)
  AVL List GmbH (AT)
  ICE Stroemungsforschung GmbH (AT)
  DTU Technical University of Denmark (DK)
  Chalmars University of Technology (SE)
  Karlsruhe Institute of Technology (DE
  University of St Andrews (UK)
  EC Joint Research Centre (NL)
Vertical integrated

## Slide 3: Project goals, targets, and milestones
The aim of the METSAPP project is to develop novel
cells and stacks based on a robust and reliable up-scale-able
metal supported technology with the following primary objectives:
Robust metal-supported cell design, ASRcell < 0.5 Ωcm2, 650ºC
Cell optimized and up-scaled to > 300 cm2 footprint
Improved durability for stationary applications, degradation < 0.25%/kh
Modular, up-scaled stack design, stack ASRstack < 0.6 Ωcm2, 650ºC
Robustness of 1-3 kW stack verified
Cost effectiveness, industrially relevance, up-scale-ability illustrated.
Stainless
steel
ScYSZ
Novel anode
Novel cathode

## Slide 4: Next Gen SOFC development
FeCr
MIEC
CGO
ScYSZ
Ceramic- Infiltrate
FeCr
MIEC
CGO
ScYSZ
Cermet - Infiltrate
EU METSOFC Cell
2008 -2011
5000 h lifetime
Mobile applications
EU METSAPP Cell
2012 – 2014
40.000 h lifetime
Stationary applications
Corrosion passivation infiltrated
Start platform
ASR: 0.27 Ωcm2 at 650 oC
Novel ”beyond state of art” concept

## Slide 5: Project concept
LEAN Development in a Complex Technology
Critical iteration (Lean spirals)
based on new acquired knowledge
Effective short cuts for rapid feedback of
information and results
Project groups (WPs) with a strong background and competences
Vertical integrated project structure (no overlap between partners)
Several links to other SOFC projects (EU, national, in-house)
Rapid cell and stack prototypes at optimal scale for test
Rapid critical optimization loops (critical iteration)
WP3
Testing
WP4
Modelling,
reliability
and
durability
WP5
Stack
development
WP6
Alloys
and coatings
WP2
Cell development
WP1
Project management
WP7&8
RTD coordination, exploitation and dissemination
Notes: 5

## Slide 6
6
Project achievements - Cell processing
Co-processing of ceramics
and metals
Multi layer tape casting
Lamination
Sintering (atmospheric avoided)
Screen printing
Infiltration (nano structuring)
4 cm2
25 cm2
144 cm2
Year
Fabrication routes
based on low-cost and upscalable processes
2010
2011
2012
300 cm2
Challenges
Strategies

## Slide 7
7
WP2 – Cell development
Tasks
2.1 Metal powder development
2.2 Development of cermet layer and nano-structured coatings
2.3 Development of novel anode designs
2.4 Integration of high performance cathodes
2.5 Integration of components to cells
2.6 Component and cell manufacturing
Novel anodes
  High electronic conductivity
  Enhanced electro-catalytic activity
  In-situ growth of catalytically active nano-particles
  Improved corrosion protection of metal components
Material and Processing R&D

## Slide 8: WP3 – Testing
Tasks
3.1 Corrosion testing
3.2 Mechanical testing
3.3 Electrochemical testing of MSCs
3.4 Analysis of the catalytic properties of MSCs
3.5 Long term stability and corrosion of MSCs
3.6 Accelerated testing on cell level
3.7 Accelerated testing on stack level
3.8 Performance monitoring of MSC-stacks
3.9 Vibration tests of MSC-stacks
New setup mechanical testing at high temperature constructed
New cermet layer = less corrosion
Novel
anode
Notes: 8

## Slide 9: Fundamental electrochemical testing
0.00
0.01
0.02
0.03
0.04
0.05
0.06
0.07
0.08
0.09
10-1
100
101
102
103
104
105
106
P1A gas diffusion in metal support
P2A
P3A
Phf ?
P2C electrochemistry cathode
f / Hz
g(f) / ∙sec
Distribution of Relaxation Times
electrochemistry anode
0.080
0.136
0.244
0.440
0.634
0.819
pH2O / atm
 cell performance data and model parameters for task 4.2/4.3
0.0
-0.1
-0.2
0
0.1
0.2
0.30
0.40
0.5
Re(Z) / ∙cm²
Im(Z) / ∙cm²
10 mHz
4 Hz
1.8 MHz
250 kHz
Identification of critical issues
METSAPP G1 cell SM 2922#2
1 cm² electrode area, H2 + H2O, air, 700°C, OCV
Impedance spectra
Improvement of basic knowledge
Notes: 9

## Slide 10: Cell performance and durability
anode infiltration A
anode infiltration B
anode infiltration C
anode infiltration D
STN/FeCr anode
Ni/CeO2 nano infiltrated
(DTU)
Materials screening
Durability

## Slide 11
Break through in new anode materials
In situ growth of metal
nanoparticles
Exolution of both
Ni and CeO2 nanoparticles
from
La0.8Ce0.1Ni0.4Ti0.6O3
D. Neagu et al., In situ growth of
nanoparticles through control
of non-stoichiometry,
Nature Chemistry, October, 2013

## Slide 12: WP4 - Modelling, reliability and durability
WP4 – Tasks
4.1 Identification of material parameters
4.2 Electrochemical Modeling of MSCs
4.3 FEM-modelling and simulation of repeat units
4.4 FEM-modelling and simulation of internal reforming in MSCs
4.5 Failure mode identification and assessment
4.6 Failure mode model development
4.7 Development of accelerated test procedures
Material parameters identified and collected in an database (AVL)
Failure mode identification and prioritization.
  A total of 17 “high priority” failure modes have been identified.
  These modes are driven by 5 classes of damage drivers.
Notes: 12

## Slide 13: From fundamental modelling to stack design optimisation
FEM-modelling of stack repeat units
combined with detailed electrochemical model
1E-5 atm
0.01
0.018
0.002
0.02 atm
pO2,cathode
pH2,anode
0.40 atm
0.31 atm
0.39
0.32
0.36
contact rib
Ucell = 0.7 V
T = 800°C
gas channel
cathode contact grid
anode contact grid
cathode
electrolyte
anode
contact rib
gas channel
(KIT)

## Slide 14: Critical failure modes
Determination of diffusion in anode (micro-structure).
Investigation of corrosion and influence on diffusion (in progress)
Next step: Understanding Creep of metal-support
Failure mode model development
FEM-modelling and simulation of internal reforming
in metal supported cells
Distribution of principal
mechanical stress in cell
Notes: 14

## Slide 15: WP5 - Stack development
More compression…
Too high compression
Too low compression…
leaky
short-circuiting
Correct procedure leads to stable operation and high performance
SoA cells, 250 hours
Stack conditioning procedure
Cells
Stack

## Slide 16: Laser welding of cells and stack components
Previous laser welding
Recent result with fiber laser
Weld in cross-section
Target: Robust seal optimized for manufacturing
Novel seal design

## Slide 17: WP6 - Alloys and coatings
Chart: Time [h]
| 0 | 1 | 24 | 72 | 168 | 500 | 3000
Uncoated | 0 | 0.05 | 0.1 | 0.189 | 0.31324 | 0.43 | 1.3069
Co 800nm | 0 | 0.24 | 0.41 | 0.528 | 0.58 | 0.8 | 1.17 | 1.8984
Ce 10/Co800nm | 0 | 0.22 | 0.54 | 0.74 | 0.89 | 0.96844
Accelerated test at 850°C in air + 3% H2O
Metal interconnects need to be coated
640nm Co are sufficient to block Cr evaporation
10nm Ce coating reduces corrosion substantially
Less corrosion  longer lifetime
Thinner scale  lower ASR values
Co coated
Co/Ce coated
2µm

## Slide 18
Large scale continuous thin film (PVD) coating production established at Sandvik (roll to roll process)
Upscaled PVD coating of strip steels
Novel cost effective coated interconnect concept

## Slide 19
Interconnectors for SOFC
  Specialized Steel – Sandvik SanergyHT
  Standard Ferritic Steel – AISI441, 430
  Continuous PVD Coatings
Bipolar plates for PEMFC
  Standard Steel – 316L, 304L
  Continuous PVD Coatings
New industrial steels and coatings

## Slide 20
Dissimination & public awareness
Schoenbein Contribution to Science Medal 2012
”For an outstanding contribution to:
Advances in Metal Supported Cells”
10th European SOFC Forum 2012
D. Neagu et al.,
In situ growth of nanoparticles through control of non-stoichiometry,
Nature Chemistry, October, 2013

## Slide 21: Cooperation and future perspectives
METSAPP
Cooperation
with other projects
FeCr
MIEC
CGO
ScYSZ
Ceramic- Infiltrate
EuroFC-Life
ProSOFC
SCOTAS
METPROCELL
DESTA
2012-2014
Demonstration network
established