## Slide 1
SOFC-Life
(256885)
L.G.J. de Haart
Forschungszentrum Jülich GmbH / IEK-9 / Germany
Joint undertaking
Fuel cells and hydrogen
Programme Review Day 2013, Brussels, 11 & 12 November 2013

## Slide 2: Project & Partnership description (1/1)
Solid Oxide Fuel Cells –
Integrating Degradation Effects into Lifetime Prediction Models
partners - industry |  |  | 
TOFC | Denmark | HTCeramics | Switzerland
EDF | France | HEXIS | Switzerland
partners - research & university |  |  | 
DTU-EC | Denmark | EPFL | Switzerland
VTT | Finnland | EMPA | Switzerland
CEA | France | ZHAW | Switzerland
FZ Jülich | Germany | Imperial College | United Kingdom
IHTE | Russia |  | 
project data | 
reference | FCH JU 256885
start date | 01/01/2011
end date | 31/12/2013
duration | 36 months
total costs | 5.700.000 €
FCH JU funding | 2.400.000 €
 | 42 %

## Slide 3
Project objectives & approach (1/3)
Objectives
Understand the details of the major SOFC continuous degradation effects
Develop models that predict single degradation phenomena
Transfer the physical-chemical models to electrochemical models
Re-assemble the single effect models to a full SRU life-time prediction model
Approach
dis-assemble the SOFC single repeating unit to model elements representing single degradation phenomena (anode and cathode compartment)
WP1: anode side phenomena
WP2: cathode side phenomena
WP3: modelling
effect details
and models
verification
validation
WP4: stack test &
model application

## Slide 4
Approach
air exposed
fuel exposed
temperature
gas composition
time
f
w/ current
w/ current
temperature
gas composition
time
current
f
changes in composition (phase)
and morphology
(post-test)
additional:
changes in resistance
(in-situ)
result
stack repeating unit
WP2: cathode side phenomena
WP1: anode side phenomena
Project objectives & approach (2/3)

## Slide 5
the stability (chemical, kinetic and morphological) of state of the art cathode materials (impacting the cathode activity)
processes at the cathode-interconnect interface (impacting electrical continuity and chemical composition of components, thus their electrochemical performance)
morphological change in the anode cermet (impacting on anode activity and electrical continuity)
nickel-steel corrosion (impacting on electrical continuity and conductivity)
WP2: cathode side phenomena
WP1: anode side phenomena
Main topics (degradation mechanism)
Project objectives & approach (3/3)

## Slide 6
Project achievements (1/9)
WP2: cathode side phenomena
WP1: anode side phenomena
Exposure tests of selected materials (combinations)
300 h
1000 h
3000 h
Test durations: 0, 300, 1000 and 3000 h. Sample extraction for post-test analyses.

## Slide 7
WP2: cathode side phenomena
Project achievements (2/9)
Post-test analysis
WP1: anode side phenomena
TPB length
Ni content
LSM interface area
YSZ interface area

## Slide 8
Project achievements (3/9)
WP2: cathode side phenomena
Cathode-Interconnect Interface
Contact resistance loss
lifetime-prediction:
3 + 0.3√t(h) mohm.cm2
Crofer H alloy, exposed 3000h, 800°C
300 h
3000 h
LSM cathode
spinel coating
scale
alloy
10 mm
10 mm

## Slide 9
Project achievements (4/9)
WP3: modeling and verification
Ni seff ele
YSZ seff ion
Active TPB length
Input from microstructure analysis
Output: prediction of electrode performance
Simulated processes
O2-
e-
O2
O2
e-
LSM
YSZ
cathode side
anode side

## Slide 10
Project achievements (5/9)
WP3: modeling and verification
Fresh LSM-8YSZ volume of
19.5 x 14.8 x 7.6 µm3
3D reconstruction by FIB/SEM tomography
19.5 m
19.4 mm
14.7 mm
25.5 mm
22.9 mm
9.5 mm
26.2 mm
Fresh Ni-8YSZ volume of
25.5 x 19.4 x 14.7 µm3
cathode side
anode side
Microstructure quantification

## Slide 11
Project achievements (6/9)
WP3: modeling and verification
The simulation provide total ASR and components of ASR
related to charge transport and TPB-reactions.
ASRtotal predictions are in good agreement with EIS-measurements
ASR-total
ASR-act
ASR-transp
After Degradation
Before Degradation
Prediction of ASR performance (before and after degradation)
X = ASR measured by EIS
Anodic polarization
Cathodic polarization
Electrode modeling in anodic and cathodic polarization
cathode side
anode side

## Slide 12
Project achievements (7/9)
WP3: modeling and verification
20 segments: DRT dataset
Fuel & Air
EIS
segmented 1-cell stack: 20 * 4 cm2 electrode segments covering the whole flow field
1000 h tests (in H2 and CH4/H2O) with periodical EIS allow to monitor local degradation processes
6 processes at well-defined frequencies identified on all 20 segments
anode charge transfer

## Slide 13
Project achievements (8/9)
WP3: modeling and verification
H2
CH4 / H2O
0h
100h
300h
600h
900h
1100h
51
73
74
70
66
64 mohm.cm2
31
32
37
56
75
80 mohm.cm2
example of local monitoring of anode charge transfer process, >1000 h, in H2 and CH4/H2O fuel
very different behavior (temporal and spatial) between the two cases

## Slide 14
Project achievements (9/9)
WP4: stack test & model application
Power density approx. 0.2 W/cm²; electrical efficiency approx. 37 % DC
Degradation approx. 4 mV, i.e. 0.5 % / 1000 h over 13000 h
Linear degradation, Fits well to the data measured on system level, as well as the model
No progressive degradation but, lab incident destroyed one, harmed the other
for Hexis ECS-type SOFC

## Slide 15
Self Assessment Summary (1/2)
Self Assessment Summary
Estimation of the probability that the project will achieve the objectives:
Understand the details of the major SOFC continuous degradation effects
  From the four themes investigated only processes at the cathode-interconnect interface can be considered to be a major contribution to the overall degradation observed in SRUs and stacks.
Objective is achieved.
Develop models that predict single degradation phenomena
  Microstructural parameters as function of operating conditions and time for cathodes and anodes have been extracted for use in the respective sub-models. Due to a limited number of experiments on the stability of the LSCF cathode as function of time no sufficient data is available for the implementation of this cathode in the model.
Objective will be partly achieved.

## Slide 16
Self Assessment Summary (2/2)
Self Assessment Summary
Estimation of the probability that the project will achieve the objectives:
Transfer the physical-chemical models to electrochemical models
  Cellular automaton model developed to predict 3D microstructure evolution, and corresponding degradation of polarization resistance, of Ni/YSZ and Ni/CGO anodes and LSM/YSZ cathodes.
Objective will be achieved for the anodes and cathodes mentioned.
Re-assemble the single effect models to a full SRU life-time prediction model
Objective will most likely be achieved.

## Slide 17
Alignment to MAIP/AIP (1/1)
Relevance to call & AIP 2009
Application area: Stationary power production and CHP
Topic: SP1-JTI-FCH.3.1: Degradation and lifetime fundamentals
SOFC-Life addresses:
basic research activities directed to degradation and lifetime fundamentals
of SOFC technology,
focusing on SOFC materials available and in industrial application today
(cf. MAIP section 3.4.3 page 15 - updated version adopted November 2011)

## Slide 18
Relationships to Earlier and Other Current Projects (1/1)
Relationship to Earlier and Other Current Projects
SOFC-Life
  builds on experiences and data collected
  in the projects Real-SOFC, SOFC600 and FlameSOFC,
  follows protocols from FCTESQA when appropriate,
  and many others in which the partners have participated.
In turn protocols from SOFC-Life are being used in the project SCORED2.

## Slide 19
Complementarity with Projects from Other Programs (1/1)
Complementarity with Projects from Other Programs
Co-funding:
• VTT: (Finish) National Fuel Cell Technology Program (TEKES)
• IHTE: (National Russian Foundation for Fundamental Research)
• DTU-EC: Danish PSO-financed program (Top-up grant)
Participation in related / complementary projects:
• see above
• DTU-EC: SOFC Accelerated (Danish, EUDP); Towards Smart Grid Ready SOFC (Danish, ForskEl); METSAPP (EU)
• FZ Jülich: German project on SOFC Degradation to start June 2014

## Slide 20
Cross-cutting, Dissemination & Exploitation Activities (1/1)
Cross-cutting & Dissemination Activities
Publications, conferences presentations
website www.sofc-life.eu

## Slide 21
Cross-cutting, Dissemination & Exploitation Activities (1/1)
Cross-cutting & Dissemination Activities
Publications, conferences presentations
website www.sofc-life.eu
Exploitation & Post-Project Activities
direct use of results by participating industries and SMEs

## Slide 22
Further RTD Activities (1/1)
Further RTD activities
Degradation models will require further refinement to make them applicable to a wider range of cell types and operating conditions.
Basic understanding should be applied to develop soundly based accelerated tests.

## Slide 23
Thank you for your attention
L.G.J. de Haart (e-mail: l.g.j.de.haart@fz-juelich.de)
Forschungszentrum Jülich GmbH / IEK-9 / Germany
Joint undertaking
Fuel cells and hydrogen
Programme Review Day 2013, Brussels, 11 & 12 November 2013

## Slide 24
Porosity (e)
Porosity &
Tortuosity (t)
Porosity &
Tortuosity &
Constrictivity (d)
Factor due to extra pathway lengths
Factor due to uneven path radii (bottlenecks)
L. Holzer et. Al., Journal of Materials Science 48(7): 2934-2952, 2013
WP3: modeling and verification
Relationship between effective transport properties and microstructure
Back-up: (1/2) Microstructure factor (M-factor)

## Slide 25
Back-up: (2/2) Microstructure factor (M-factor)
WP3: modeling and verification
Relationship between effective transport properties and microstructure investigated with virtual materials testing
a) More than 100 virtual microstructures with specific properties (e, b, t) are created with stochastic geometry.
b) The virtual microstructures cover a wide range of microstructure parameters (e, b, t) :
c) Finite Element Modeling based on meshes from virtual microstructures is used to calculate the corresponding effective conductivities seff
d) The database from virtual testing provides the relationship between microstructure parameters (e,t,b) and effective transport properties (seff).
Using statistical error minimization leads to the following relationship:
This expression can be used to describe effective electric and ionic conductivities as well as gas phase diffusivity
‘M-factor’